ISSN 1392-3196

Žemdirbystė / Zemdirbyste-Agriculture, t. 95, Nr. 4 (2008), p. 81–96

UDK  633.521:[631.3:631.56

## ĮVAIRAUS  TANKUMO  LINŲ  PASĖLIO  PLUOŠTO  IŠEIGOS  IR KOKYBĖS  POKYČIAI  KLOJĖJIMOSI  METU

##### Marius BALČIŪNAS, Zofija JANKAUSKIENĖ

Lietuvos žemdirbystės institutas

Linininkų g. 3, Upytė, Panevėžio r. sav.

El. paštas: marius@lzi.lt, soja@upyte.lzi.lt

###### Santrauka

2005–2007 m. Lietuvos žemdirbystės instituto Upytės bandymų stotyje vykdyti įvairaus tankumo linų pasėlio stiebelių klojėjimosi tyrimai. Linų priešsėlis – žieminiai rugiai, sėti po antrųjų naudojimo metų daugiamečių žolių. Dirvožemis – giliau karbonatingas giliau glėjiškas rudžemis (Endocalcari-Endohypogleyic Cambisol) – bandymo vykdymo metais buvo šarmiškas, fosforingas ir didelio fosforingumo, vidutinio kalingumo, mažo ir vidutinio humusingumo. Sėti pluoštiniai linai ‛Hermes’ sėjamąja NODET 7 įvairiomis normomis nuo 10 iki 34 mln. daigių sėklų ha-1. Šio bandymo tikslas – nustatyti optimalų pluoštinių linų pasėlio tankumą pagal linų klojėjimosi metu nustatytus pluošto išeigos bei jo kokybės rodiklius. Didžiausia klojėtų linų brukto pluošto išeiga nustatyta laukeliuose, kur pasėlio tankumas buvo apie 2 100 vnt. m-2 augalų (sėta 30 mln. daigių sėklų ha-1). Didžiausias klojėto pluošto stiprumas bei lankstumas daugeliu atvejų nustatytas tankesniame pasėlyje (1 540–2 380 vnt. m-2), o mažesnis – retesniame (700–1 260 vnt. m-2). 2005–2006 m. tyrimų duomenimis, ilgėjant klojėjimosi trukmei pluošto lankstumas klojėjimosi metu mažai kito, o 2007 m. – mažėjo.

2005–2007 m. tyrimų duomenimis, pagal pluošto išeigos bei kokybės rodiklius optimalus linų pasėlio tankumas buvo apie 1 820–2 100 vnt. vnt. m-2 (sėjant 26–30 mln. mln. ha-1 sėklų).

Reikšminiai žodžiai: dinamika, klojėjimas, lankstumas, pluoštiniai linai, pluošto kokybiniai rodikliai, pluošto išeiga, stiprumas.

ISSN 1392-3196

Zemdirbyste-Agriculture, vol. 95, No. 4 (2008), p. 81–96

UDK  633.521:[631.3:631.56

### THE  CHANGES  IN  FLAX  FIBRE  CONTENT  AND  QUALITY  DURING THE  DEW-RETTING  OF  FLAX  STANDS  OF  VARIOUS  DENSITIES

M. Balčiūnas, Z. Jankauskienė

Lithuanian Institute of Agriculture

Summary

Experiments were conducted during 2005–2007 at the LIA’s Upytė Research Station. Flax was preceded by winter rye sown after perennial grasses of the second year of use. The soil of the experimental site is Endocalcari-Endohypogleyic Cambisol, with a pHKCL value of 7.3–7.5, humus content 1.53–2.31%, available P2O5 164–275 mg kg-1, and available K2O 125–136 mg kg-1. The fibre flax variety ‛Hermes’ was sown by a sowing machine NODET at 7 different sowing rates ranging from 10 to 34 million viable seeds ha-1 (crop density ranged from approx. 700 to 2,380 plants m-2). The trial was replicated three times. The flax long fibre tenacity was measured by the Fibre Dynamometer DK-60 in units kilogram force (kg F).

The aim of the study was to estimate the optimal flax crop density according to the parameters of flax fibre content and quality, which were determined when investigating the dynamics of flax dew-retting in the treatments of different crop densities. Having summarised the data from 3 years, it was found out that the optimal flax crop density for fibre quantity and quality parameters could be considered 1,820–2,100 plants m-2 (treatments with seed rate of 26 and 30 million ha-1). The most flexible fibre in majority cases was obtained at crop density of 2,380 plants m-2 (when sowing 34 million ha-1 seed), and the lowest fibre flexibility was produced in the treatments at a crop density of 700–980 plants m-2 (with a sowing rate of 10 and 14 million seeds ha-1). A similar situation was with fibre tenacity: the best flax fibre tenacity was obtained at a crop density of 2,100–2,380 plants m-2 (when sowing 30–34 million seeds ha-1) and the lowest fibre tenacity was determined in the treatments at a crop density of 700–980 plants m-2 (sowing rate of 10 and 14 million seeds ha-1). The highest fibre content and fibre yield in most cases were obtained at a crop density of 2,100 plants m-2.

Key words: dynamics, dew-retting, fibre content, fibre flax, quality of flax fibre, fibre flexibility, fibre tenacity.